PRODUCT DATA SHEET

TECHNOFLUID FOOD GRADE GEAR OIL

Commercial / Pack Name: ISO VG 220 / 320

Product Description

- Premium food-grade gear oils formulated from highly refined white mineral base oils and food-grade performance additives.

- Designed for enclosed gear systems where incidental food contact may occur.

- Excellent load carrying capability and anti-wear performance.

- Superior oxidation stability for extended lubricant service life.

- Available in ISO VG 220 and ISO VG 320 viscosity grades.

Key Performance Benefits

- Excellent protection against gear wear and micropitting.

- Outstanding oxidation and thermal stability.

- High load carrying capacity.

- Excellent rust and corrosion protection.

- Long service life with reduced maintenance.

Applications

- Enclosed gearboxes in food and beverage processing plants.

- Bakery, dairy, beverage and meat processing equipment.

- Pharmaceutical and cosmetic manufacturing machinery.

- Food packaging and conveyor drive systems.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Excellent EP and anti-wear performance

- High oxidation stability

- Excellent rust and corrosion protection

- Low foaming tendency

- Long lubricant life

Typical Characteristics

| Characteristics | ISO VG 220 | ISO VG 320 |
| --- | --- | --- |
| Appearance | Clear | Clear |
| Density @29.5°C | 0.870 | 0.875 |
| K.V @40°C cSt | 220 | 320 |
| Viscosity Index | 95 | 95 |
| Pour Point °C | -9 | -6 |
| Flash Point (COC) °C | 250 | 260 |