PRODUCT DATA SHEET

FOOD GRADE HYDRAULIC OIL

Commercial / Pack Name: ISO VG 22 / 32 / 46 / 68 / 100

Product Description

- Premium food-grade hydraulic oils formulated from highly refined white mineral base oils and food-grade performance additives.

- Designed for hydraulic systems where incidental food contact may occur.

- Excellent oxidation stability and long service life.

- Outstanding anti-wear protection, rust prevention and corrosion resistance.

- Available in ISO VG 22, 32, 46, 68 and 100 viscosity grades.

Key Performance Benefits

- Excellent anti-wear performance for hydraulic pumps and valves.

- High oxidation and thermal stability.

- Good water separation and filterability.

- Superior rust and corrosion protection.

- Long equipment life with reduced maintenance.

Applications

- Food processing plants.

- Beverage manufacturing facilities.

- Pharmaceutical and cosmetic industries.

- Packaging and bottling equipment.

- Hydraulic systems requiring food-grade lubricants.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Excellent anti-wear protection

- High oxidation stability

- Good demulsibility

- Excellent air release

- Low foaming tendency

- Long service life

Typical Characteristics

| Characteristics | ISO VG 22 | ISO VG 32 | ISO VG 46 | ISO VG 68 | ISO VG 100 |
| --- | --- | --- | --- | --- | --- |
| Appearance | Clear | Clear | Clear | Clear | Clear |
| Density @29.5°C | 0.845 | 0.850 | 0.855 | 0.860 | 0.865 |
| K.V @40°C cSt | 22 | 32 | 46 | 68 | 100 |
| Viscosity Index | 100 | 100 | 100 | 100 | 100 |
| Pour Point °C | -18 | -18 | -15 | -12 | -9 |
| Flash Point (COC) °C | 200 | 210 | 220 | 230 | 240 |