PRODUCT DATA SHEET

SCREW AIR COMPRESSOR OIL / AIR COMPRESSOR OIL

Commercial / Pack Name: Screw Compressor Oil 32 / 46 / 68 , Air Compressor Oil 100 / 150 / 220

Product Description

- Premium compressor lubricants formulated from highly refined base oils and advanced additives.

- Designed for rotary screw and reciprocating air compressors.

- Excellent oxidation and thermal stability.

- Low deposit formation for clean compressor operation.

- Superior anti-wear, rust and corrosion protection.

Key Performance Benefits

- Extended oil service life.

- Excellent air release and anti-foam performance.

- Minimizes sludge and varnish.

- Reduces maintenance costs.

- Reliable protection under severe operating conditions.

Applications

- Rotary screw compressors.

- Reciprocating air compressors.

- Industrial compressed air systems.

- Manufacturing, textile, mining and engineering industries.

INDUSTRY PERFORMANCE CHARACTERISTICS

- High oxidation stability

- Excellent thermal stability

- Rapid air release

- Low foaming tendency

- Excellent wear protection

- Long service life

Typical Characteristics

| Characteristics | SC 32 | SC 46 | SC 68 | AC 100 | AC 150 | AC 220 |
| --- | --- | --- | --- | --- | --- | --- |
| Appearance | Clear | Clear | Clear | Clear | Clear | Clear |
| Density @29.5°C | 0.845 | 0.850 | 0.858 | 0.865 | 0.870 | 0.875 |
| K.V @40°C cSt | 32 | 46 | 68 | 100 | 150 | 220 |
| Viscosity Index | 100 | 100 | 100 | 98 | 98 | 95 |
| Pour Point °C | -18 | -18 | -15 | -12 | -9 | -6 |
| Flash Point (COC) °C | 210 | 220 | 230 | 235 | 235 | 235 |