PRODUCT DATA SHEET

TECHNOFLUID TRACTOR ENGINE OIL

Commercial / Pack Name: 15W-40 CH-4 / 20W-40 CF

Product Description

- Premium tractor engine oils formulated with high quality base oils and advanced additive technology.

- Designed for naturally aspirated and turbocharged diesel tractor engines.

- Excellent detergency, dispersancy and oxidation stability.

- Provides outstanding protection against wear, rust and corrosion.

- Available in 15W-40 CH-4 and 20W-40 CF grades.

Key Performance Benefits

- Excellent engine cleanliness and sludge control.

- Superior wear protection for extended engine life.

- High thermal and oxidation stability.

- Reliable performance under heavy agricultural operations.

- Reduces maintenance and oil consumption.

Applications

- Agricultural tractors and farm equipment.

- Diesel engines operating in tractors, harvesters and allied machinery.

- Suitable where API CH-4 or API CF performance is recommended.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Excellent soot handling

- Superior wear protection

- High oxidation stability

- Good corrosion resistance

- Extended engine life

Typical Characteristics

| Characteristics | 15W-40 CH-4 | 20W-40 CF |
| --- | --- | --- |
| Appearance | Bright & Clear | Bright & Clear |
| Density @29.5°C | 0.860 | 0.880 |
| K.V @100°C cSt | 14.8 | 14.5 |
| Viscosity Index | 140 | 130 |
| TBN | 9.5 | 7.0 |
| Flash Point (COC) °C | 225 | 220 |
| Pour Point °C | -27 | -21 |