PRODUCT DATA SHEET

TECHNOFLUID WHITE OIL ISO VG 12 / 32 / 100

Commercial / Pack Name: ISO VG 12 / 32 / 100

Product Description

- Highly refined, colourless, odourless and chemically stable white mineral oils manufactured from premium quality base oils.

- Excellent purity with low aromatic content and high oxidation stability.

- Provides outstanding lubricity, water-white appearance and long service life.

- Non-staining and suitable where clean lubrication is essential.

- Available in ISO VG 12, ISO VG 32 and ISO VG 100 viscosity grades.

Key Performance Benefits

- High oxidation resistance and thermal stability.

- Excellent colour stability and low volatility.

- Good rust protection and anti-foam characteristics.

- Safe for applications requiring clean, non-staining mineral oil.

- Consistent performance over a wide operating temperature range.

Applications

- Textile machinery and fibre processing.

- Pharmaceutical, cosmetic and personal care manufacturing (technical-grade applications as specified).

- Food packaging machinery and general clean lubrication applications where appropriate.

- Plastic, rubber and chemical processing.

- General industrial lubrication requiring colourless mineral oil.

INDUSTRY PERFORMANCE CHARACTERISTICS

- High purity and water-white appearance

- Excellent oxidation stability

- Low odour and non-staining performance

- Reliable viscosity characteristics

- Long service life

Typical Characteristics

| Characteristics | ISO VG 12 | ISO VG 32 | ISO VG 100 |
| --- | --- | --- | --- |
| Appearance | Water White | Water White | Water White |
| Density @29.5°C | 0.805 -0.85 | 0.830 -0.845 | 0.865 |
| K.V @40°C cSt | 11-14 | 30-32 | 95-105 |
| Viscosity Index | 95 | 98 | 100 |
| Pour Point °C | -9 | -9 | -6 |
| Flash Point COC °C | >160 | 210 | >250 |