PRODUCT DATA SHEET

FOOD GRADE GREASE EP 2 (H1)

Commercial / Pack Name: FOOD GRADE GREASE EP 2 (H1)

Product Description

- Premium H1 food-grade grease formulated from highly refined white base oils, food-grade thickener and performance additives.

- Designed for bearings and equipment where incidental food contact may occur.

- Excellent water resistance, mechanical stability and oxidation resistance.

- Provides outstanding wear protection and corrosion resistance.

- Suitable for a wide range of food processing applications.

Key Performance Benefits

- Excellent load carrying capability.

- Outstanding resistance to water washout.

- Superior oxidation and mechanical stability.

- Excellent rust and corrosion protection.

- Long service life with reduced relubrication frequency.

Applications

- Food and beverage processing plants.

- Bakery, dairy and meat processing equipment.

- Conveyor bearings, rollers and packaging machinery.

- Pharmaceutical and cosmetic manufacturing equipment.

- General anti-friction bearings operating in food processing environments.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Excellent water resistance

- High mechanical stability

- Outstanding anti-wear performance

- Excellent corrosion protection

- Long grease life

Typical Characteristics

| Characteristics | EP 2 (H1) |
| --- | --- |
| Appearance | White |
| NLGI Grade | 2 |
| Thickener | Aluminium Complex |
| Base Oil Viscosity @40°C | 220 cSt |
| Worked Penetration | 265-295 |
| Dropping Point | 260°C Min |
| Operating Temperature | -20°C to +160°C |