PRODUCT DATA SHEET

REAR AXLE OIL (JCB & OFF-HIGHWAY EQUIPMENT)

Commercial / Pack Name: Rear Axle Oil (JCB) SAE 80W / SAE 90

Product Description

- Premium rear axle oil formulated with high quality mineral base oils and advanced extreme pressure (EP) additives.

- Designed for rear axles, differentials and final drives used in JCB construction equipment and off-highway machinery.

- Provides outstanding protection under heavy shock loads and severe operating conditions.

- Excellent oxidation stability, rust and corrosion protection for extended service life.

- Suitable for equipment operating in construction, mining and earthmoving applications.

Key Performance Benefits

- Excellent extreme pressure and anti-wear performance.

- High load carrying capability for heavily loaded gears.

- Reduces gear scuffing, pitting and wear.

- Excellent thermal and oxidation stability.

- Protects against rust, corrosion and foam formation.

Applications

- JCB backhoe loaders and construction equipment.

- Rear axle assemblies and final drives.

- Differentials of earthmoving and off-highway equipment.

- Suitable where EP gear lubricants meeting API GL-5 or equipment manufacturer recommendations are specified.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Outstanding EP protection

- Excellent load carrying capability

- Superior wear protection

- Excellent oxidation stability

- Extended component life

Typical Characteristics

| Characteristics | SAE 80W | SAE 90 |
| --- | --- | --- |
| Appearance | Bright & Clear | Bright & Clear |
| Density @29.5°C | 0.890 | 0.895 |
| K.V @40°C cSt | 75 | 180 |
| Viscosity Index | 105 | 95 |
| Flash Point (COC) °C | 210 | 220 |
| Pour Point °C | -27 | -12 |