PRODUCT DATA SHEET

RUBBER PROCESS OIL

Commercial / Pack Name: RPO 710 / ELASTOL 245 / ELASTOL 541

Product Description

- Premium rubber process oils manufactured from highly refined mineral base oils.

- Developed to improve processing efficiency and compound dispersion in rubber manufacturing.

- Excellent compatibility with natural and synthetic rubber compounds.

- Provides good thermal stability, low volatility and consistent processing performance.

- Available in RPO 710, ELASTOL 245 and ELASTOL 541 grades.

Key Performance Benefits

- Improves filler dispersion and processability.

- Enhances flexibility and finished product quality.

- Excellent oxidation and thermal stability.

- Low aromatic content and consistent viscosity.

- Reduces energy consumption during mixing and processing.

Applications

- Tyre and tube manufacturing.

- Rubber hoses, belts, footwear and moulded rubber goods.

- Automotive rubber components.

- General natural and synthetic rubber compounding.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Excellent compatibility with rubber polymers

- Good thermal stability

- Low volatility

- Consistent processing characteristics

- Improved compound flow

Typical Characteristics

| Characteristics | RPO 710 | ELASTOL 245 | ELASTOL 541 |
| --- | --- | --- | --- |
| Appearance | Dark green | Yellow clear | Yellow clear |
| Density @29.5°C | 0.940 | 0.865 | 0.850 |
| K.V @40°C cSt | 70 | 30-32 | 18-23 |
| Flash Point (COC) °C | 220 | 210 | 175 |
| Pour Point °C | -6 | -3 | -3 |
| Aniline Point °C | 90 | 95 | 100 |

RUBBER PROCESS OIL

Commercial / Pack Name: RPO 710 / ELASTOL 245 / ELASTOL 541

Product Description

- Premium rubber process oils manufactured from highly refined mineral base oils.

- Designed to improve processing, filler dispersion and finished rubber properties.

- Excellent compatibility with natural and synthetic rubber compounds.

- Good thermal stability and low volatility for consistent processing.

- Available in RPO 710, ELASTOL 245 and ELASTOL 541 grades.

Key Performance Benefits

- Improves processability and compound flow.

- Enhances filler dispersion and flexibility.

- Consistent viscosity and excellent thermal stability.

- Low aromatic loss during processing.

- Reliable performance for a wide range of rubber products.

Applications

- Tyres and tubes.

- Footwear and conveyor belts.

- Rubber hoses and moulded goods.

- Automotive rubber components.

- General natural and synthetic rubber compounding.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Excellent compatibility with rubber polymers

- Consistent processing performance

- Low volatility

- Good thermal stability

- Improved filler dispersion

Typical Characteristics

| Characteristics | RPO 710 | ELASTOL 245 | ELASTOL 541 |
| --- | --- | --- | --- |
| Appearance | Brown | Brown | Brown |
| Density @29.5°C | 0.890 | 0.900 | 0.905 |
| K.V @40°C (cSt) | 70 | 245 | 541 |
| Aniline Point (°C) | 90 | 95 | 100 |
| Copper Corrosion (100°C, 3 h) | 1a | 1a | 1a |
| Asphaltenes (% wt) | Nil | Nil | Nil |
| Polar Compounds (% wt) | <10 | <10 | <10 |
| Aromatics (% wt) | 28 | 22 | 18 |
| Saturates (% wt) | 72 | 78 | 82 |
| Flash Point (COC) °C | 220 | 245 | 260 |
| Pour Point (°C) | -6 | -6 | -3 |