PRODUCT DATA SHEET

TECHNOFLUID TURBINE OILS

Commercial / Pack Name: ISO VG 32 / 46 / 68 / 100

Product Description

- Premium turbine oils formulated from highly refined base oils and advanced anti-oxidant technology.

- Designed for steam, gas and hydro turbine lubrication systems.

- Excellent oxidation stability and long service life.

- Superior rust, corrosion and foam protection.

- Available in ISO VG 32, 46, 68 and 100 grades.

Key Performance Benefits

- Outstanding oxidation and thermal stability.

- Excellent water separation characteristics.

- Rapid air release and low foaming tendency.

- Reliable rust and corrosion protection.

- Extended oil drain intervals and reduced maintenance.

Applications

- Steam turbines.

- Gas turbines.

- Hydroelectric turbines.

- Industrial circulating lubrication systems.

- Power generation and process industries.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Excellent oxidation stability

- High demulsibility

- Rapid air release

- Low foaming tendency

- Long service life

Typical Characteristics

| Characteristics | ISO VG 32 | ISO VG 46 | ISO VG 68 | ISO VG 100 |
| --- | --- | --- | --- | --- |
| Appearance | Clear | Clear | Clear | Clear |
| Density @29.5°C | 0.845 | 0.850 | 0.855 | 0.865 |
| K.V @40°C cSt | 32 | 46 | 68 | 100 |
| Viscosity Index | 100 | 100 | 100 | 98 |
| Pour Point °C | -18 | -15 | -12 | -9 |
| Flash Point (COC) °C | 210 | 220 | 230 | 240 |