PRODUCT DATA SHEET

TECHNOFLUID FOOD GRADE WHITE OIL

Commercial / Pack Name: ISO VG 32 / 46 / 68 / 100

Product Description

- Premium food-grade white mineral oils manufactured from highly refined, colourless and odourless base oils.

- Formulated for applications where incidental food contact may occur.

- Excellent oxidation stability and chemical purity.

- Non-staining, non-toxic appearance with outstanding colour stability.

- Available in ISO VG 32, 46, 68 and 100 viscosity grades.

Key Performance Benefits

- High purity and water-white appearance.

- Excellent oxidation and thermal stability.

- Low volatility and long service life.

- Excellent rust protection and corrosion resistance.

- Suitable for clean lubrication applications.

Applications

- Food and beverage processing plants.

- Bakery, dairy and confectionery industries.

- Pharmaceutical and cosmetic manufacturing.

- Food packaging machinery and conveyor systems.

- General clean lubrication and process oil applications.

INDUSTRY PERFORMANCE CHARACTERISTICS

- Water-white appearance

- High oxidation stability

- Excellent colour stability

- Low odour and non-staining

- Long service life

Typical Characteristics

| Characteristics | ISO VG 32 | ISO VG 46 | ISO VG 68 | ISO VG 100 |
| --- | --- | --- | --- | --- |
| Appearance | Water White | Water White | Water White | Water White |
| Density @29.5°C | 0.845 | 0.850 | 0.855 | 0.860 |
| K.V @40°C cSt | 32 | 46 | 68 | 100 |
| Viscosity Index | 100 | 100 | 100 | 100 |
| Pour Point °C | -12 | -12 | -9 | -6 |
| Flash Point (COC) °C | 210 | 220 | 230 | 245 |