PRODUCT DATA SHEET

MARINE ENGINE OIL

Commercial / Pack Name: SAE 30 (TBN 12/15), SAE 40 (TBN 20/30/40), 15W-40, Cylinder Oil 50 TBN, Cylinder Oil 70 TBN, System Oil SAE 30

Product Description

- Premium marine lubricants formulated from high quality base oils and advanced additive technology.

- Designed for trunk piston and marine diesel engines operating under severe service conditions.

- Excellent detergency, dispersancy and oxidation stability.

- Provides outstanding wear, rust and corrosion protection.

- Available for main engine, cylinder lubrication and marine system lubrication.

Key Performance Benefits

- Controls piston deposits and sludge formation.

- Excellent acid neutralization through optimized TBN levels.

- Superior oxidation and thermal stability.

- Extends engine life and minimizes wear.

- Reliable performance in coastal and ocean-going vessels.

Applications

- Medium and high-speed marine diesel engines.

- Fishing boats, cargo vessels and marine auxiliary engines.

- Crosshead engine cylinder lubrication (Cylinder Oils).

- Marine crankcase/system lubrication (System Oil SAE 30).

INDUSTRY PERFORMANCE CHARACTERISTICS

- High detergency and dispersancy

- Excellent wear protection

- Superior corrosion resistance

- High thermal and oxidation stability

- Extended oil service life

Typical Characteristics

| Characteristics | SAE30 TBN12/15 | SAE40 TBN20/30/40 | 15W-40 | Cyl 50 | Cyl 70 | System SAE30 |
| --- | --- | --- | --- | --- | --- | --- |
| Appearance | Bright | Bright | Bright | Bright | Bright | Bright |
| Density @29.5°C | 0.865 | 0.870 | 0.870 | 0.890 | 0.890 | 0.865 |
| K.V @40°C cSt | 100 | 150 | 110 | 220 | 240 | 100 |
| Viscosity Index | 98 | 98 | 135 | 95 | 95 | 98 |
| Flash Point °C | 230 | 235 | 225 | 240 | 245 | 230 |
| TBN | 12/15 | 20/30/40 | 12 | 50 | 70 | 5 |