PRODUCT DATA SHEET

## TECHNOFLUID P 165

## Product Description

## TECHNOFLUID P 165 is a premium-quality Rubber Process Oil manufactured from highly refined API Group II base oils. It is specially developed for use in rubber compounding and processing operations where excellent thermal stability, high flash point, and consistent viscosity are required.

## The product exhibits excellent compatibility with a wide range of elastomers and processing chemicals while providing improved filler dispersion, enhanced processability, and uniform mixing. Its high purity, low volatility, and transparent appearance make it suitable for modern rubber manufacturing processes.

### Typical Characteristics

| Property | Test Method | Typical Value |
| --- | --- | --- |
| Product Type | — | Rubber Process Oil |
| Base Oil Type | — | API Group II |
| Appearance | Visual | Clear & Transparent |
| Color | Visual | Water White to Pale |
| Density @ 15°C | ASTM D4052 | 0.860 g/cm³ |
| Kinematic Viscosity @ 40°C | ASTM D445 | 120–130 cSt |
| Flash Point (COC) | ASTM D92 | >260°C |
| Pour Point | ASTM D97 | Below -6°C (Typical) |
| Sulphur Content | ASTM D4294 | Low |
| Volatility | ASTM D5800 | Low |
| Oxidation Stability | ASTM D943 | Excellent |
| Aromatic Content | — | Very Low |
| Compatibility | — | Suitable for most natural and synthetic rubber compounds |

## Key Benefits

## - Manufactured from premium API Group II base oils

## - Excellent processability during rubber mixing

## - Improves dispersion of fillers and additives

## - High flash point for safer plant operation

## - Excellent thermal and oxidation stability

## - Low volatility, minimizing oil loss during processing

## - Consistent viscosity for uniform batch quality

## - Clean, transparent appearance

## - Low aromatic content compared to conventional process oils

## - Suitable for modern rubber compounding operations

## Typical Applications

## TECHNOFLUID P-165 is recommended for use in:

## - Tyre manufacturing

## - Rubber hoses

## - Conveyor belts

## - Rubber mats

## - Footwear compounds

## - Automotive rubber components

## - Molded rubber goods

## - Extruded rubber products

## - General-purpose rubber compounding

## Handling & Storage

## - Store in clean, dry and covered conditions.

## - Keep containers tightly closed.

## - Protect from moisture and contamination.

## - Avoid prolonged exposure to direct sunlight.

## - Recommended storage temperature: 5°C to 40°C.

## Health & Safety

## Avoid prolonged skin contact. Wear appropriate protective equipment during handling. Refer to the latest Safety Data Sheet (SDS) before use.

## Disclaimer

## The information contained herein is based on current manufacturing data and is believed to be accurate. Typical values are not to be construed as product specifications and may vary slightly within normal manufacturing tolerances. Users should evaluate the product's suitability for their specific application before use.